Prediction of Compressive Strength of Concrete Based on Mix Proportion

ABSTRACT

Density and Strength of concrete are one of the most utilized parameter in the consideration for its proposed use. The requirement for concrete of high strength always leads to its high density which often instigates a correlation between the strength and the densities. Though, the corresponding outcome of a concrete density and strength depend on the constituent material, the proportion of the mix also is of utmost necessity. This research was experimentally carried out to investigate and provide a mathematical relationship between the density and the compressive strength of common concrete mixes (1:11/2, 1:2:4 and 1:3:6).

Seventy-two (72) concrete cube samples were cast and the result of the density and strength for the different mix ratio was obtained for 7, 14, 21 and 28 curing days. The result was interacted among the constituent to generate a simple mathematical equation to predict the strength of a concrete at each of the curing days. Mat-Lab software was used to generate the non-linear equation which has Cement, Sand and Granite ratio, water/cement ratio, curing age and density as the independent variable to give strength as a dependent variable.

The result of the predicted strength is related to the actual strength for each of the curing ages and a residual strength of less than 1N/mm2 were obtained for 80%, 71%, 100% and 96%,  were gotten for the 7, 14, 21 and 28days curing ages. These agree with the regression coefficient for each of the curing ages of 0.9763, 0.9718, 0.9953, and 0.9927 respectively for the 7, 14, 21 and 28 curing days. Also, the prediction of concrete’s 28days strength from the 7days density was in agreement with its actual strength with regression of 0.9934.

It can be concluded that there is non-linear correlation between the density and strength of concrete and also between 7days and 28days density and strength. In future, it is recommended that the generated equation should be used for strength prediction.

Table 1: Compressive Strength and Density of concrete

| Input Parameters |  |  |  |  |  | Output Parameters |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cement (kg/m3) | Sand (kg/m3) | Granite (kg/m3) | Age (days) | Water (kg/m3) | w/c | Slump (mm) | Density (kg/m3) | Compressive strength (N/mm2) |
| 263 | 788.3 | 1576.7 | 7 | 170.95 | 0.65 | 6 | 2014 | 4.89 |
| 263 | 788.3 | 1576.7 | 7 | 170.95 | 0.65 | 6 | 2122 | 7.56 |
| 263 | 788.3 | 1576.7 | 7 | 170.95 | 0.65 | 6 | 2044 | 6.89 |
| 263 | 788.3 | 1576.7 | 7 | 170.95 | 0.65 | 6 | 2252 | 7.11 |
| 263 | 788.3 | 1576.7 | 7 | 170.95 | 0.65 | 6 | 2074 | 5.56 |
| 263 | 788.3 | 1576.7 | 7 | 170.95 | 0.65 | 6 | 2163 | 7.78 |
| 263 | 788.3 | 1576.7 | 14 | 170.95 | 0.65 | 6 | 2341 | 10.67 |
| 263 | 788.3 | 1576.7 | 14 | 170.95 | 0.65 | 6 | 2163 | 8.22 |
| 263 | 788.3 | 1576.7 | 14 | 170.95 | 0.65 | 6 | 2341 | 9 |
| 263 | 788.3 | 1576.7 | 14 | 170.95 | 0.65 | 6 | 2222 | 10.78 |
| 263 | 788.3 | 1576.7 | 14 | 170.95 | 0.65 | 6 | 2281 | 11.11 |
| 263 | 788.3 | 1576.7 | 14 | 170.95 | 0.65 | 6 | 2222 | 10.67 |
| 263 | 788.3 | 1576.7 | 21 | 170.95 | 0.65 | 6 | 2315 | 11.67 |
| 263 | 788.3 | 1576.7 | 21 | 170.95 | 0.65 | 6 | 2252 | 10.44 |
| 263 | 788.3 | 1576.7 | 21 | 170.95 | 0.65 | 6 | 2222 | 12 |
| 263 | 788.3 | 1576.7 | 21 | 170.95 | 0.65 | 6 | 2370 | 11.97 |
| 263 | 788.3 | 1576.7 | 21 | 170.95 | 0.65 | 6 | 2251 | 10.67 |
| 263 | 788.3 | 1576.7 | 21 | 170.95 | 0.65 | 6 | 2311 | 11.58 |
| 263 | 788.3 | 1576.7 | 28 | 170.95 | 0.65 | 6 | 2311 | 13.26 |
| 263 | 788.3 | 1576.7 | 28 | 170.95 | 0.65 | 6 | 2394 | 12.92 |
| 263 | 788.3 | 1576.7 | 28 | 170.95 | 0.65 | 6 | 2370 | 13.64 |
| 263 | 788.3 | 1576.7 | 28 | 170.95 | 0.65 | 6 | 2393 | 13 |
| 263 | 788.3 | 1576.7 | 28 | 170.95 | 0.65 | 6 | 2322 | 11.98 |
| 263 | 788.3 | 1576.7 | 28 | 170.95 | 0.65 | 6 | 2400 | 14.2 |
| 338 | 675.9 | 1351.7 | 7 | 219.7 | 0.65 | 15 | 2133 | 8.79 |
| 338 | 675.9 | 1351.7 | 7 | 219.7 | 0.65 | 15 | 2385 | 10 |
| 338 | 675.9 | 1351.7 | 7 | 219.7 | 0.65 | 15 | 2252 | 9.33 |
| 338 | 675.9 | 1351.7 | 7 | 219.7 | 0.65 | 15 | 2281 | 9.56 |
| 338 | 675.9 | 1351.7 | 7 | 219.7 | 0.65 | 15 | 2163 | 9.89 |
| 338 | 675.9 | 1351.7 | 7 | 219.7 | 0.65 | 15 | 2281 | 11.11 |
| 338 | 675.9 | 1351.7 | 14 | 219.7 | 0.65 | 15 | 2281 | 10.5 |
| 338 | 675.9 | 1351.7 | 14 | 219.7 | 0.65 | 15 | 2193 | 9.33 |
| 338 | 675.9 | 1351.7 | 14 | 219.7 | 0.65 | 15 | 2252 | 10.33 |
| 338 | 675.9 | 1351.7 | 14 | 219.7 | 0.65 | 15 | 2222 | 11.13 |
| 338 | 675.9 | 1351.7 | 14 | 219.7 | 0.65 | 15 | 2263 | 12.12 |
| 338 | 675.9 | 1351.7 | 14 | 219.7 | 0.65 | 15 | 2389 | 11.61 |
| 338 | 675.9 | 1351.7 | 21 | 219.7 | 0.65 | 15 | 2370 | 13.33 |
| 338 | 675.9 | 1351.7 | 21 | 219.7 | 0.65 | 15 | 2370 | 12.67 |
| 338 | 675.9 | 1351.7 | 21 | 219.7 | 0.65 | 15 | 2370 | 12.57 |
| 338 | 675.9 | 1351.7 | 21 | 219.7 | 0.65 | 15 | 2233 | 11.89 |
| 338 | 675.9 | 1351.7 | 21 | 219.7 | 0.65 | 15 | 2311 | 11.56 |
| 338 | 675.9 | 1351.7 | 21 | 219.7 | 0.65 | 15 | 2341 | 12.22 |
| 338 | 675.9 | 1351.7 | 28 | 219.7 | 0.65 | 15 | 2311 | 15.44 |
| 338 | 675.9 | 1351.7 | 28 | 219.7 | 0.65 | 15 | 2352 | 16.56 |
| 338 | 675.9 | 1351.7 | 28 | 219.7 | 0.65 | 15 | 2411 | 17.23 |
| 338 | 675.9 | 1351.7 | 28 | 219.7 | 0.65 | 15 | 2370 | 16.21 |
| 338 | 675.9 | 1351.7 | 28 | 219.7 | 0.65 | 15 | 2408 | 16.14 |
| 338 | 675.9 | 1351.7 | 28 | 219.7 | 0.65 | 15 | 2341 | 16.96 |
| 466 | 699 | 1398 | 7 | 302.9 | 0.65 | 35 | 2504 | 22.44 |
| 466 | 699 | 1398 | 7 | 302.9 | 0.65 | 35 | 2459 | 19.33 |
| 466 | 699 | 1398 | 7 | 302.9 | 0.65 | 35 | 2459 | 17.78 |
| 466 | 699 | 1398 | 7 | 302.9 | 0.65 | 35 | 2519 | 20 |
| 466 | 699 | 1398 | 7 | 302.9 | 0.65 | 35 | 2467 | 20.67 |
| 466 | 699 | 1398 | 7 | 302.9 | 0.65 | 35 | 2501 | 22.01 |
| 466 | 699 | 1398 | 14 | 302.9 | 0.65 | 35 | 2489 | 24.67 |
| 466 | 699 | 1398 | 14 | 302.9 | 0.65 | 35 | 2519 | 21.33 |
| 466 | 699 | 1398 | 14 | 302.9 | 0.65 | 35 | 2626 | 21.56 |
| 466 | 699 | 1398 | 14 | 302.9 | 0.65 | 35 | 2519 | 21.56 |
| 466 | 699 | 1398 | 14 | 302.9 | 0.65 | 35 | 2430 | 24.89 |
| 466 | 699 | 1398 | 14 | 302.9 | 0.65 | 35 | 2578 | 20.44 |
| 466 | 699 | 1398 | 21 | 302.9 | 0.65 | 35 | 2548 | 26.44 |
| 466 | 699 | 1398 | 21 | 302.9 | 0.65 | 35 | 2607 | 27.33 |
| 466 | 699 | 1398 | 21 | 302.9 | 0.65 | 35 | 2578 | 28 |
| 466 | 699 | 1398 | 21 | 302.9 | 0.65 | 35 | 2430 | 25.78 |
| 466 | 699 | 1398 | 21 | 302.9 | 0.65 | 35 | 2460 | 26.89 |
| 466 | 699 | 1398 | 21 | 302.9 | 0.65 | 35 | 2459 | 26 |
| 466 | 699 | 1398 | 28 | 302.9 | 0.65 | 35 | 2726 | 29.93 |
| 466 | 699 | 1398 | 28 | 302.9 | 0.65 | 35 | 2548 | 28 |
| 466 | 699 | 1398 | 28 | 302.9 | 0.65 | 35 | 2607 | 30.2 |
| 466 | 699 | 1398 | 28 | 302.9 | 0.65 | 35 | 2430 | 29.24 |
| 466 | 699 | 1398 | 28 | 302.9 | 0.65 | 35 | 2489 | 30 |
| 466 | 699 | 1398 | 28 | 302.9 | 0.65 | 35 | 2578 | 29.78 |